NCHRP 20-7

Proposed Research Need Statement

AASHTO Subcommittee on Bridges and Structures

Chair, Gregg Fredrick, WY

July 2014

TITLE

Efficient Fatigue Design Guidelines for Hand holes in Highway Sign, Luminaire and Traffic Signal Structures

RESEARCH PROBLEM STATEMENT

The fatigue design guidelines for reinforced and unreinforced hand holes in the current 6th Edition of the AASHTO Standard Specifications for Structural Supports for Highway Signs, Luminaires and Traffic Signals provides for a clear hand hole opening of maximum 40% of the tube or pole diameter, which is about 13% of the pole perimeter. In addition, a corner radius of 30 to 50% of the clear opening width is suggested; and the thickness of the hand hole frames are suggested to be ¼ in. and 1 in. respectively for sign/signal and high level luminaire support structures. These criteria were developed based on the research performed under NCHRP Project 10-70: Cost-effective Connection Details for Highway Sign, Luminaire and Traffic Signal Structures, where full size specimens having reinforced and unreinforced hand holes were fatigue tested under the most critical stress conditions. A stress concentration factor (SCF) of 4.0 is specified based on the suggested hand hole configuration.

While the suggested hand hole configuration covers most design situations, in certain cases particularly for smaller diameter poles in the respective class of structures (sign/signal support and high level luminaire support), the required hand hole exceeds 40% of the pole diameter. A limited review of the currently fabricated structures reveal that the high level luminaire structures in the range of 55 to 100 ft. height are mostly affected, where openings as large as 87% of the pole diameter (or about 28% of the pole perimeter) have been used. In sign and signal support structures, poles of 10 in. diameter or less are the most affected. These are a significant population of the structures in the inventory. In other situations, multiple openings may be needed on a particular section that cumulatively exceeds 40% of the pole diameter.

In such situations, where the reinforced or un-reinforced hand hole does not meet the AASHTO provisions, the specifications allow use of alternative hole and cutout configurations as approved by the Owner based on sound engineering practices. The specifications provide guidance in Appendix D for assessing these holes and cutouts based on advanced Finite Element Analyses and/or laboratory testing, which can require significant expert effort and add to the structure cost. Alternatively, the pole sizes need to be increased to meet the specification provisions, which can significantly add to the structure cost. In addition to fatigue resistance, the effect of larger hand holes on the ultimate strength of the structure is not well known. The prevalent design practice is to provide an equivalent frame area for the opening, which in some cases may not be adequate. Research is needed to develop efficient design guidelines for hand holes with openings larger than 40% that would ensure cost-effective and safe structures.

LITERATURE SEARCH SUMMARY

Fatigue cracking at the toe of the hand hole frame-to-pole weld has been reported for a few structures in-service, where the cracks have mostly initiated at the weld toe of the rounded corner of the hand hole and propagated into the pole (Dexter 2004). A literature search of domestic and international publications revealed that the performance of hand hole details in the subject structures were only investigated under NCHRP Project 10-70 (Roy et al. 2011). The cracking mode observed in the field, however, could not be replicated in the laboratory specimens tested under NCHRP Project 10-70. The specimens included round 13 in. diameter poles representing sign and signal supports, and multi-sided 24 in. diameter poles representing high level luminaire supports. An approximately 5×7½ in. hand hole (total opening) was included in the sign and signal structure specimens. Both reinforced and unreinforced hand holes were tested. The hand hole in the high level lighting support structure specimens was reinforced and followed the existing Wyoming DOT standard drawings, which was the only standard of the subject structures available in 2006, having a clear opening of 12×32 in. The frames of the reinforced hand holes in the sign signal structure specimen and the high level luminaire structure specimens were ¼ in. and 1 in. thick respectively. Only the sign and signal structure specimens developed fatigue cracking. In the reinforced hand holes, the crack grew from the inherent lack of fusion of the weld root at the hand hole corner, and propagated normal to the weld axis into the pole wall. For unreinforced hand holes, fatigue cracks developed in the pole base metal initiating at the hand hole corner. Advanced Finite Element Analyses (FEA) showed that stress concentration existed at the rounded corners of the hand holes as the in plane stress in the pole wall deviated around the hand hole. The observed fatigue cracking in the laboratory specimens was consistent with the principal stress field around the hand hole and the weld detail classification. Constant amplitude fatigue thresholds (CAFT) of 16 ksi and 7 ksi were specified against fatigue crack growth from the weld root and the weld toe respectively. Based on FEA of the specimens, a SCF of 4.0 was specified for the hand hole configuration, which was found to be primarily influenced by the pole diameter and thickness, the opening configuration (size and geometry), and the hand hole frame thickness.

RESEARCH OBJECTIVE

The objectives of the proposed research are as follows:

(1) to establish fatigue resistance of several hand hole configurations including the effects of critical geometric and fabrication parameters; and

(2) to develop fatigue design guidelines for hand holes of different configurations including revisions to the AASHTO Specification for Structural Supports for Highway Signs, Luminaires and Traffic Signals.

The research is expected to involve the following major tasks:

Task 1: Literature Review

Task 2: Identify Critical Parameters affecting the Fatigue Resistance of Hand Hole Connections

Task 3: Conduct Parametric Studies

Task 4: Conduct Experimental Studies of Selected Details

Task 5: Develop Design Guidelines

Task 6: Propose Revisions to the AASHTO Specifications

ESTIMATE OF PROBLEM FUNDING AND RESEARCH PERIOD

Recommended Funding: $96,000

Research Period: 12 months

URGENCY, PAYOFF POTENTIAL, AND IMPLEMENTATION

The recently implemented 6th Edition of the AASHTO Standard Specifications for Structural Supports for Highway Signs, Luminaires and Traffic Signals promote cost-effective design of the subject structures; however, potential exists for inefficient design and significant cost increase of a subset of these structures due to the limitations imposed by the hand hole design provisions. While fatigue cracking of reinforced and unreinforced hand holes has been reported in service, their occurrence is relatively rare. In addition, there is no evidence of adverse performance of hand holes that exceed the AASHTO suggested configurations. As such, a more comprehensive design guides need to be developed for hand holes of different geometric configurations. Since, many states are gearing up to implement the latest specifications, including transitioning to the recently approved LRFD Specifications for the subject structures, where the subject provisions are identical to the Standard specifications, possibility exists for costly and inefficient standard designs of a significant population of these structures. The proposed research is urgently needed to prevent this situation and further strengthen the existing design specifications. It is envisaged that the proposed research will help in building an inventory of robust and cost-effective sign and signal structures that will perform with minimum maintenance over their design life. This will help in efficient and more productive use of the over-encumbered infrastructure funds.

The research results will be easy to incorporate within the framework of the current AASHTO fatigue design specifications, which are already implemented. The research will develop specification verbiage, which can be balloted as an interim addition to the existing specification.

The proposed research will address the HSCOBS Strategic Plan objectives of Extending Service Life and Maintaining and Enhancing the AASHTO Specifications.

CONTACT PERSON

Mr. Barry Benton, P.E.

State Bridge Engineer

Delaware Department of Transportation

Chair, SCOBs Technical Committee T12 for

Structural Supports for Signs, Luminaires and Traffic Signals

References:

Dexter, R.J., (2004). Investigation of cracking of high-mast lighting towers. Iowa Department of Transportation, Ames, IA.

Roy, S., Park, Y.C., Sause, R., Fisher, J.W., and Kaufmann, E.J. (2011). Cost-effective connection details for highway sign, luminaire and traffic signal structures. NCHRP web-only Document 176. Washington, D.C.: Transportation Research Board.